Table 3. Calculated equilibrium phase fractions (mol%) at 1200 °C, the solution-treatment temperature. The benchmark alloy cannot be evaluated in PrecHiMn-04, which contains no Ni.

| Alloy | mpea-02b | PrecHiMn-04 | mc_fe v2.059 |
| --- | --- | --- | --- |
| benchmark alloy | 100 α | – | 100 α |
| LLM-alloy | 71.1 α + 28.9 γ | 64.5 α + 35.5 γ | 61.9 α + 38.1 γ |
| LLM-alloy, C removed | 100 α | 100 α | 100 α |