Table 1. Chemistries (in wt.%) of the two alloys as measured by inductively coupled plasma atomic emission spectroscopy (ICP-AES). Carbon was measured by ASTM E1019. Elements present at less than 0.01 wt% are not listed.

| Element | AI-alloy |  | Omori-alloy |  |
| --- | --- | --- | --- | --- |
|  | nominal | actual | nominal | actual |
| Fe | 54.5 | 55.83 | 47.08 | 46.51 |
| Mn | 32.3 | 31.78 | 36.43 | 36.49 |
| Al | 6.4 | 6.24 | 7.9 | 8.00 |
| Ni | 4.6 | 4.81 | 8.59 | 8.94 |
| Si | 2.2 | 1.11 | - | <0.01 |
| C | 0.1 | 0.105 | - | 0.01 |
| P | - | - | - | 0.06 |