|  | Fe (at%) | Mn(at%) | Al(at%) | Ni(at%) | C (PPM) | Si(at%) |
| --- | --- | --- | --- | --- | --- | --- |
| 697-6 | 50 | 30 | 12 | 4 | 1000 | 4 |
| 697-7 | 43.5 | 34 | 15 | 7.5 |  |  |

Request a 5-6 pounds ingot based on Al suggestion: (6/4/25)

54.5Fe-32.3Mn-6.4Al-2.2Si-4.6Ni-0.1C (wt%) or 50Fe-30Mn-12Al-4Si-4Ni (at%)-1000ppm C

Added 1730-Fe, 1025-Mn, 203-Al, 69.9-Si, 146-Ni and 3.2-C (all in grams), melt at 1650C for 30 minute before pour into a water cooled Cu mode.

Only ~ 2pounds get poured into the mode. Hole is too small.

X-ray gun two beam testing results (wt%)

| Al | Al +/- | Si | Si +/- | Mn | Mn +/- | Fe | Fe +/- | Ni | Ni +/- |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6.19 | 0.7 | 1.97 | 0.12 | 26.37 | 0.25 | 60.41 | 0.48 | 5.06 | 0.11 |
| 7.83 | 0.71 | 2.16 | 0.12 | 27.08 | 0.25 | 58.32 | 0.48 | 4.52 | 0.1 |

EDM cut two .500” rod, homogenized at 1000C/16HRS in argon

Hot roll at 850C

7/26/25: second trial, hot roll at 850C without homogenization to ~.175” square , cold swaged to .173” round. …. Draw to .0142”. heat treating at 12000c to achieve bamboo structure. Frankie has the process notes.

8/31/25: 2nd process to .0508”, grind to .152”, annealed at 1000C/2FPM, draw to .081”, 1000c/2fpm, argon, draw to .0508”. AGG heat treatment and testing, see Frank for processing notes

Two cycle AGG, 1200C/30m WQ+900C/15m, 1200C/30m WQ+900C/15m, 1200c30m wq

Three cycle AGG: 1200C/30m WQ+900C/15m, 1200C/30m WQ+900C/15m, 1200C/30m WQ+900C/15m 1200C60m wq

7/30/25: duplicate famous composition that was found working before (RD0697-7)

43.5Fe-34Mn-15Al-7.5Ni (at%) or 47.08Fe-36.43Mn-7.9Al-8.59Ni (wt%)

(analyzed chemistry: 46.5Fe-36.5Mn-8Al-8.94Ni (wt%)-0.01C)

Melted in VIM, lots of voids, remelt on Arcast, cast .600” dia. 6” long rod,

9/6/25: hot swage at 900c to .475”, hot roll at 900C to .210” square. Anneal at 900c/1min, cold swaged to .200” round. GRIND TO .170”.

- 9/13/25, .170” as grund, .162”, .144”, heavily galled, etch to .134”

- 1000C/2FPM, Hydrogen F72, .128”, .120”,  .114”, .102”, .091, .081”, .072”, .064”.

- Annealed at 1200C/4fpm, H2, wire very brittle, couldn’t draw

- 1000C/4FPM Ar, .0605”, 0.057”, .0508”, .045”, .0403”  (appears that 1200C is not a good annealing temperature…)

- Continue draw to .0253”

- 1200C30m F72, 900C/10m F30, Argon. Repeat 5 times. Material is easily stretched. (9/29/25)

- 1200C/1HR F72 Argon.

10/11/25: Both alloy 697-6 (.014”) and 7(.025”), seal inside a quartz tube, 1200c/30m Ar atmosphere, swaitch to cold zone for 10 minutes, 1200/30, cold zone for10 minutes, 1200C/30m, cold zone 10m, 1200c/30m, water quench.