Dear Editor,

Please find enclosed our second revision of JMRT-D-26-06169R1, Experimental Validation of an LLM-Hypothesized Fe-Mn-Al-Ni-Si-C Alloy: Phase Stability Governs the Absence of Super-elasticity. Reviewers 1 and 2 closed their reviews (Reviewer 2 recommending acceptance); Reviewer 3 raised eight further points, and this revision answers each of them. The response to Reviewer 3 quotes every point verbatim and states where the manuscript changed.

Three things we should draw to your attention directly.

- A correction of our own. In preparing this revision we found that the CALPHAD scripts used for Revision 1 had silently omitted the liquid phase from two of the three thermodynamic databases, so the α-solvus temperatures quoted in Revision 1 (≈1340 and ≈1390 °C) were artifacts. Every calculation has been re-run with the liquid phase present, the superseded results archived, and every affected sentence rewritten (abstract; Secs. 2.6, 3.4, 4.1, 4.2, 4.4, 5; Fig. 9 redrawn; new Table 4). The corrected result is stronger and simpler — in all three databases the LLM-alloy begins to melt before any single-phase α field opens — but the numbers in Revision 1 were wrong, and we say so in the response (Reviewer 3, point 6).

- One attribution corrected in Sec. 3.5. The 40-minute-anneal elongation quoted in Revision 1 (11.0% falling to 1.4%) came from a rod test record that, on re-examination of the raw files, belongs to the benchmark heat. It is withdrawn and replaced by the LLM-alloy’s own record for that condition (25.5% falling to 0.8%), which supports the same conclusion. Every tensile record of the LLM-alloy in the prolonged-anneal and cyclically treated conditions is now presented directly in a new Fig. 10, plotted from the raw load–extension exports with each test’s gauge stated (Reviewer 3, point 7).

- Two measurements requested by Reviewer 3 are outstanding. Reviewer 3 asks for a loading–unloading–heating test on the cyclically treated condition (point 7) and a direct measurement of the martensite-start temperature (point 8). Neither could be completed within the revision period. The manuscript states plainly that neither has been performed, and it no longer uses the untested condition or the inferred Ms to carry any conclusion. Both measurements have been requested at Fort Wayne Metals. Should you consider either necessary for a decision, we would ask for a short extension for that item alone, and would report the result as a bound in the terms set out in the response.

The other changes are textual: the conclusions of the submitted manuscript are tabulated as held, corrected, or withdrawn and replaced (point 1); the contribution is stated as three specific claims and the pre-screening check is explicitly not claimed as new (point 2); the cyclic heat-treatment schedules are stated per specimen, with the chronology and the intent (point 3); the gauge length is given per dataset from the instrument records, and the load-frame record of the Fig. 3 tests has been located (point 4); and every conclusion is bounded to the conditions reported, with a three-level statement of what was measured, what is calculated, and what is not claimed (point 5).

We upload three response documents, one per reviewer. The marked-up manuscript shows every change against the Revision-1 file the reviewers read.

This work is original, is not under consideration elsewhere, and all authors have approved the revised version.

Sincerely, on behalf of all authors,

Frank Y. Cai School of Engineering Technologies, Purdue University West Lafayette, Indiana 47907, USA cai485@purdue.edu