Table 2. Mechanical properties of the LLM-alloy (0.36 mm wire) after heat treatment for 1 minute at different temperatures, tested on a 127 mm gauge (Sec. 2.4); E is the apparent modulus from crosshead strain. Each data point is the average of three samples; the uncertainty is one standard deviation.

| Temp. (°C) | σ₀.₂ (MPa) | UTS (MPa) | Elong. (%) | E (GPa) |
| --- | --- | --- | --- | --- |
| As drawn | 1587.9 ± 63.7 | 1936.6 ± 19.2 | 2.0 ± 0.1 | 138.5 ± 5.1 |
| 600 | 1908.0 ± 29.2 | 2254.3 ± 27.3 | 2.2 ± 0.1 | 155.7 ± 2.2 |
| 700 | 1635.3 ± 35.9 | 1876.0 ± 9.4 | 2.2 ± 0.0 | 156.1 ± 2.0 |
| 800 | 1151.1 ± 11.3 | 1208.6 ± 5.2 | 26.1 ± 1.7 | 151.4 ± 2.9 |
| 900 | 936.3 ± 5.5 | 1081.5 ± 2.5 | 30.6 ± 0.6 | 153.1 ± 1.4 |
| 1000 | 674.8 ± 1.5 | 977.8 ± 7.7 | 33.0 ± 0.3 | 156.0 ± 2.0 |
| 1100 | 570.6 ± 10.3 | 970.3 ± 16.5 | 29.1 ± 0.6 | 161.9 ± 3.6 |
| 1200 | 518.7 ± 11.8 | 968.3 ± 21.4 | 25.6 ± 1.2 | 161.2 ± 5.5 |