Table 4. Calculated single-phase α field in the solid state and calculated solidus (°C). “None” means that liquid appears before the last γ dissolves. Values are read from a 10 °C temperature grid and carry that resolution; the solidus is the first temperature at which the liquid fraction exceeds 0.5%.

| Alloy | mpea-02b | PrecHiMn-04 | mc_fe v2.059 |
| --- | --- | --- | --- |
| benchmark alloy | α 1140–1320; solidus ≈1325 | – | α 950–1360; solidus ≈1370 |
| LLM-alloy | none; solidus ≈1295 | none; solidus ≈1295 | none; solidus ≈1240 |
| LLM-alloy, C removed | α 1150–1370; solidus ≈1375 | α 1160–1290; solidus ≈1295 | α 1130–1240; solidus ≈1245 |