# Online Resource 2 — Supplementary tables for: Absence of Superelasticity in an LLM-Hypothesized Fe-Mn-Al-Ni-Si-C Alloy: Tensile, Synchrotron and CALPHAD Assessment

Frank Y. Cai, S. Cai, X. Wang, J. Yan

Corresponding author: cai485@purdue.edu

Table S1 lists every specimen behind the figures and tables of the article; Table S2 lists every thermodynamic calculation. Section (Sec.), figure and table numbers refer to the article.

## Table S1. Specimen and record register

Heats: RD0697-6 = LLM-alloy; RD0697-7 = benchmark alloy. Diameters are the values entered in the test record for that specimen (nominal wire size in brackets where it differs). “Identity” states what on the primary record ties the specimen to its alloy: a heat number printed per specimen, a composition label printed per specimen, or the heat number under which the whole report is filed. Tensile tests: room temperature, displacement control, strain = crosshead extension / gauge length without extensometry, stress from the recorded diameter (Sec. 2.4). “Cyclic tension” = loading in successive increments of nominally 1% strain with an unloading after each, up to ≈8–12% strain or earlier fracture, then loading to fracture, at a crosshead speed of 0.25 in min⁻¹ where the record states it (M2, M3, M6–M13). Unknown cells are marked not recorded.

(a) Chemistry

| ID | Alloy (heat) | Material analyzed | Method | n | Appears in | Identity |
| --- | --- | --- | --- | --- | --- | --- |
| C1 | LLM (RD0697-6) | finished 0.36 mm wire | ICP-AES (Al, Fe, Mn, Ni, Si); C and O by ASTM E1019 | 1 | Table 1; Secs. 2.1, 2.6 | heat number (RD0697-6) on laboratory certificate |
| C2 | benchmark (RD0697-7) | as cast | ICP-AES with residual-element scan, Fe by difference; C and O by ASTM E1019 | 1 | Table 1; Secs. 2.1, 2.6 | heat reference RD0697 (no suffix) and material designation Fe-Mn-Al-Ni on laboratory certificate |

(b) Mechanical tests

| ID | Alloy (heat) | Form; measured diameter | Condition | Test | Gauge length | n | Appears in | Identity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| M1 | LLM (RD0697-6) | wire (0.36 mm); not recorded per specimen | as drawn | cyclic tension | 127 mm | 3 | Table 2 | laboratory summary table |
| M2 | LLM (RD0697-6) | wire; plotted specimens 0.352–0.359 mm | 1 min (nominal) at 600, 700, 800, 900, 1000, 1100, 1200 °C; plotted specimens strand passes at 4 ft min⁻¹ | cyclic tension | 127 mm | 3 per condition (Table 2); 1 per panel (Fig. 2a–g) | Table 2; Fig. 2a–g; Secs. 3.2, 4.3 | heat number on report file (plotted specimens); laboratory summary table (means) |
| M3 | LLM (RD0697-6) | wire; 0.348 mm | 1200 °C/1 min + 200 °C/3 h | cyclic tension | 127 mm | 1 | Fig. 2h; Secs. 3.2, 3.5 | heat number on report file |
| M4 | LLM (RD0697-6) | wire; 0.352 mm | 1200 °C/1 min | loading to 3%, unloading, heating to ≈200 °C, reloading | 127 mm | 1 | Fig. 3a | heat number per specimen on instrument record |
| M5 | benchmark (RD0697-7) | wire; 0.536 mm | 1200 °C/1 min | as M4 | 127 mm | 1 | Fig. 3b | heat number per specimen on instrument record |
| M6 | LLM (RD0697-6) | wire; 0.358 mm | 1200 °C/40 min static hold + 200 °C/3 h | cyclic tension | 127 mm | 1 | Fig. 10a; Sec. 3.5 | heat number on report file |
| M7 | LLM (RD0697-6) | wire (0.36 mm); 0.325 mm | 1200 °C/80 min | cyclic tension | 127 mm | 1 | Fig. 10b; Sec. 3.5 | heat number on report file |
| M8 | LLM (RD0697-6) | wire; 0.358 mm | 1250 °C/5 min and 1250 °C/20 min static holds | cyclic tension | 127 mm | 1 each | Sec. 2.2 (text only) | heat number on report file |
| M9 | LLM (RD0697-6) | rod; 1.29 mm | two-cycle 1200 ↔ 900 °C (Sec. 2.2) | cyclic tension | 127 mm | 2 | Fig. 10c; Sec. 3.5 | heat number on report file |
| M10 | LLM (RD0697-6) | rod; 1.06 mm | three-cycle 1200 ↔ 900 °C + 200 °C/3 h | cyclic tension | 127 mm | 1 | Fig. 10d; Sec. 3.5 | heat number on report file |
| M11 | LLM (RD0697-6) | rod; 1.06 mm | three-cycle 1200 ↔ 900 °C + 200 °C/3 h | cyclic tension | 6.0 mm | 1 | Fig. 10e; Sec. 3.5 | heat number on report file; condition printed per specimen |
| M12 | LLM (RD0697-6) | wire; 0.356 mm | quartz-tube cycle, 4 × 1200 °C/30 min, water quench (Sec. 2.2) | cyclic tension | 25.4 mm | 1 | Fig. 10f; Sec. 3.5 | composition label per specimen on instrument record (label reads “3 time”; hold count from the processing log); fracture strain taken from the raw load–extension export (last point above 20% of peak load, 0.261 in), the instrument summary’s 51.3% including post-fracture crosshead travel |
| M13 | LLM (RD0697-6) | wire; 0.356 mm | 1300 °C cyclic exposure (hold count not recorded) | cyclic tension | 25.4 mm | 1 | Sec. 2.2 (text only) | composition label per specimen on instrument record (label reads “3 time”) |

(c) Metallography

| ID | Alloy (heat) | Form | Condition | Technique | n | Appears in | Identity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| G1 | LLM (RD0697-6) | wire | 1200 °C/1 min strand pass | optical | 1 | Fig. 1a | alloy and condition in image label |
| G2 | LLM (RD0697-6) | not recorded | 1200 °C/1 min | SEM, EDS | 1 | Fig. 1b; Sec. 3.1 | not recorded |
| G3 | LLM (RD0697-6) | wire (section ≈0.3 mm) | 1200 °C/40 min | optical | 1 | Fig. 1c | section width against scale bar |
| G4 | LLM (RD0697-6) | wire (section 330 µm) | quartz-tube cycle (Sec. 2.2) | optical | 1 | Fig. 1d | composition label in image label; processing log; section width against scale bar |
| G5 | LLM (RD0697-6) | rod, ≈1 mm (section 868 µm) | three-cycle 1200 ↔ 900 °C | optical | 1 | Sec. 3.5 (text only) | alloy in image label; section width against scale bar |
| G6 | LLM (RD0697-6) | rod, ≈1.08 mm | three-cycle 1200 ↔ 900 °C + 200 °C/3 h | stereomicroscope, surface | 1 | Sec. 3.5 (text only) | condition in image label; width against scale bar |
| G7 | benchmark (RD0697-7) | wire, 0.64 mm (section ≈570–630 µm) | cyclic treatment of Sec. 2.2 (which of the two benchmark runs: not recorded) | optical | 1 | Sec. 3.5 (text only) | composition label in image label; section width against scale bar |

(d) Synchrotron diffraction (SSRF BL12SW, λ = 0.12587 Å, one or two detector frames per specimen)

| ID | Alloy (heat) | Form | Condition | Analysis | Tensile record of the deformed specimen | Appears in | Identity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| X1 | LLM (RD0697-6) | wire | 1200 °C/1 min, undeformed | Rietveld (MAUD 2.33, three-phase, E-WIMV) | – | Figs. 4a, 5a, 6a, 7; Sec. 3.3 | beamline sample list (Sam5; frame NO7286) |
| X2 | LLM (RD0697-6) | wire | 1200 °C/1 min, unloaded from 10% strain | Rietveld (as X1) | not recorded | Figs. 4b, 5b, 6a | beamline sample list (Sam6; frame NO7280) |
| X3 | benchmark (RD0697-7) | wire | 1200 °C/1 min, undeformed; two frames | qualitative (Sec. 3.3) | – | Figs. 4c, 6b | beamline sample list (Sam7; frames NO7271, NO7274) |
| X4 | benchmark (RD0697-7) | wire | 1200 °C/1 min, unloaded from 8% strain; two frames | qualitative | not recorded | Figs. 4d, 6b | beamline sample list (Sam8; frames NO7265, NO7268) |
| X5 | LLM (RD0697-6) | ≈1 mm rod | three-cycle 1200 ↔ 900 °C, final 1200 °C/1 h WQ; two frames | qualitative | – | Fig. 8 | beamline sample list (Sam1, “3-cycle AGG, 1200C/1h WQ”; frames NO7325, NO7328) |

## Table S2. Calculation register

All calculations: pycalphad 0.11.2, 1 atm, liquid phase included, databases as distributed in the pycalphad open multicomponent-database collection. Elements a database does not carry were omitted and the remainder renormalized (Sec. 2.6). “pdens” is pycalphad’s starting-grid density in points per degree of freedom. Starting grids were pdens 500 (mpea-02b, PrecHiMn-04) or 2000 (mc_fe). In the high-temperature bands of the step diagrams (mpea-02b: benchmark from 1300 °C, LLM-alloy from 1250 °C, C-free LLM-alloy from 1350 °C; PrecHiMn-04: LLM-alloy from 1150 °C, C-free LLM-alloy from 1280 °C; all to 1400 °C) the lowest-Gibbs-energy state across density ladders spanning pdens 300–4000 was retained. The Ni scans (K4, K5) and A2-window runs (K6, K7) were not arbitrated.

| ID | Calculation | Database (elements) | Compositions (at%, unless stated) | Temperatures | pdens | Appears in |
| --- | --- | --- | --- | --- | --- | --- |
| K1 | step diagrams | mpea-02b (Al, C, Fe, Mn, Ni) | benchmark Fe–34.1Mn–15.2Al–7.8Ni–0.04C; LLM Fe–29.8Mn–11.9Al–4.2Ni–0.45C; LLM with C removed | 400–1400 °C, 10 °C | 500 (ladder 300–4000 in arbitrated bands) | Fig. 9; Tables 3, 4; Sec. 3.4 |
| K2 | step diagrams | PrecHiMn-04 (Al, C, Fe, Mn, Si) | LLM Fe–29.8Mn–11.9Al–2.04Si–0.45C; LLM with C removed | 400–1400 °C, 10 °C | 500 (ladder 300–4000 in arbitrated bands) | Tables 3, 4; Sec. 3.4 |
| K3 | step diagrams | mc_fe v2.059 (Al, C, Fe, Mn, Ni, P, Si) | benchmark Fe–34.1Mn–15.2Al–7.8Ni–0.10P–0.04C–0.02Si; LLM Fe–29.8Mn–11.9Al–4.2Ni–2.04Si–0.45C; LLM with C removed | 400–1400 °C, 10 °C | 2000 | Tables 3, 4; Sec. 3.4 |
| K4 | Ni scan | mpea-02b (Al, C, Fe, Mn, Ni) | LLM with Ni 4.2 → 7.8 at% in 0.4 at% steps, Fe balance, C at 0.45 at% and C removed | 1000–1400 °C, 10 °C; 400–950 °C, 25 °C | 500 | Secs. 3.4, 4.2 |
| K5 | Ni scan, endpoints | mc_fe v2.059 (Al, C, Fe, Mn, Ni, Si) | Ni 4.2 and 7.8 at%, with and without C | as K4 | 2000 | Sec. 3.4 |
| K6 | A2-window points and Al scan | mpea-02b (Al, C, Fe, Mn, Ni; Si omitted) | wt%: measured and nominal melt; A2 midpoint Fe–25Mn–10Al–4.5Ni–2.5Si–0.2C; ferritic corner Mn 20, Al 12, Si 4, Ni 6, C 0.1; austenitic corner Mn 30, Al 8, Si 1, Ni 3, C 0.3; Al 6.4 → 12.0 wt% in 0.7 wt% steps on the nominal melt composition. Each point with C as stated and with C removed | 1000–1400 °C, 10 °C | 500 | Secs. 3.4, 5 |
| K7 | A2-window points | mc_fe v2.059 (Al, C, Fe, Mn, Ni, Si) | the named points of K6 (not the Al scan), with C as stated and with C removed | 1000–1400 °C, 10 °C | 2000 | Secs. 3.4, 5 |
| K8 | phase compositions (partitioning between α and γ) | mpea-02b, PrecHiMn-04 and mc_fe v2.059, phase sets as K1–K3 | LLM as in K1–K3 | 1200 °C | as K1–K3 (500, 500, 2000) | Sec. 3.4 |

Phases entered:

- mpea-02b: LIQUID, B2_BCC (ordered partition of A2_BCC), A1_FCC, KAPPA_E21, CEMENTITE_D011, M23C6_D84, M7C3_D101, M5C2, GRAPHITE_A9, CBCC_A12, CUB_A13, HCP_A3, SIGMA_D8B, AL8FE5_D82, AL8MN5_D810, AL13FE4, AL5FE2, AL2FE, AL3NI2_D513, AL3NI_D011, AL3NI5, AL4NI3, AL71FE5NI24, AL11MN4_HT, AL11MN4_LT, AL12MN, AL6MN_D2H, AL4MN_MU, AL4MN_LAMBDA.

- PrecHiMn-04: LIQUID, BCC_4SL (A2/B2/D0₃), A1_FCC, KAPPA_E21, CEMENTITE_D011, M23C6_D84, M7C3_D101, M5C2, GRAPHITE_A9, CBCC_A12, CUB_A13, HCP_A3, AL8FE5_D82, AL8MN5_D810, AL13FE4, AL5FE2, AL2FE, AL12MN, AL6MN_D2H, AL11MN4_HT, AL11MN4_LT, FE2SI, FESI2_H, FESI2_L, M3SI, M5SI3_D88, FE8SI2C, SIGMA_D8B.

- mc_fe v2.059: LIQUID, BCC_A2, BCC_B2, FCC_A1, K_CARB (κ), CEMENTITE, M23C6, M7C3, KSI_CARBIDE, M5C2, GRAPHITE, BETA_MN, ALPHA_MN, HCP_A3, G_PHASE; M2P and M3P in K3 only.